SOL-GEL SYNTHESIS OF Fe-CONTAINING SILICA SPHERICAL POWDERS

A.A.Boiko, E.N.Poddenezhny*, V.A.Boiko*, L.V.Sudnik**

# Gomel State Technical University, 48 October Av., 246746 Gomel, Belarus,

# E-mail: kenko@gpi.gomel.by

## *Gomel State University, 104 Sovietskaya St., 246699 Gomel, Belarus

**Reserch Institute of Powder Metallurgy, 41, Platonova St., 220600 Minsk, Belarus

Iron-containing silica glasses and nanocomposites can be used as ferromagnetic materials and color filters [1, 2]. Utilization of the sol-gel process for synthesis of silica glass is preferable because its low sintering temperature and high efficiency. Incorporation of fluorine into xerogel simultaneously with Fe-ions reduces bubble formation upon consolidation by sintering and result in the formation of Fe-containing clusters in the network of silica-gel glass.

The Fe-doped spherical powders for a formation of glasses and composites were prepared by sol-gel process, modified in the part of TEOS hydrolysis technique. The flowchart of novel sol-gel process shows in figure.

The process of monolithic silica spherical powders incorporates the hydrolysis of tetraethylorthosilicate in the system Si(C2H5O)4 – H2O – NH4F – (CH2)6N4, addition of ferric sel into sol, gelation. After gelation the wet gel was dried slowly from room temperature up to 1000C in the period 1-2 days. The following thermo-treatment of Fe-containing xerogel in air at the temperature 6000C lead to formation of silica glass-like powders of spherical form. The following thermo-treatment of Fe-containing xerogels in air at the temperatures 12000C lead to formation of silica glass-like powders containing ~200-250 ppm of OH- groups.

REM investigation demonstraite spherical formes of particles sized up to 1.0-1.5 mkm of diameter. The models of (MeFx)n nanosized clusters in the structure of silica gel-matrixes were proposed after studying of morphology and optical parameters silica spherical powders. The cold izostatic pressing (CIP) procedure for preparation of Fe3+-containing silica powders results in light-scattered materials of brown colour.

### REFERENCES

- T.Akiyama, E.Tanigawa, T.Ida, Chemistry Letters, 1986, 723.

- P.S.Shultz, J. Am. Ceram. Soc., 1974, 57, 309.

# Text boxes

FeCl3

TEOS, HMTA, H2O, NH4F

, H2O, NH4F

#### Drying

#### Gelation

Hydrolysis of TEOS

#### Sintering

#### Xerogel powders

Silica spherical powders

Fe-containing glass