OPTICAL MATERIALS PREPARED BY THE SOL-GEL PROCEDURE

Andrzej M. K³onkowski*1, Stefan Lis2, Marek Pietraszkiewicz3, Zbigniew Hnatejko2, Iwona Sza³kowska1 and Marian Elbanowski2

1 Faculty of Chemistry , University of Gdañsk, 80-952 Gdañsk, Poland, e-mail: aklonk@chemik.chem.univ.gda.pl

2 Faculty of Chemistry, A. Mickiewicz University, Poznañ, Poland

3 Institute of Physical Chemistry, Polish Academy of Sciences, Warszawa, Poland

Our studies are focused on luminescent materials based on the antenna effect and prepared by the sol-gel method. These materials are composed of Eu(III) complex (luminescence centre) entrapped in xerogel matrix. Luminescence intensity and lifetime depend on efficiency of energy transfer from the absorption centre (ligand) to the emission centre (central ion) and on concentration of O-H oscillators (quenchers) surrounding the central ion. In this study such luminescence properties as emission intensity and lifetime were improved by modifying the coordination environment of the central ion, changing anion group and matrix. Results of the experiments concerning the coordination sphere show that a cryptand ligand with aromatic groups and a second aromatic ligand, settle efficient action the antenna effect and isolate the central ion from each efficient quenchers as e.g. water molecules. Luminescence properties depend also on anion in the Eu(III) complex salt and a type of matrix material as well as concentration of water and OH groups in the matrix. The prepared luminescent materials have been tested for their photochemical stability under conditions of continuous UV irradiation.